218

RRR-1.1-14

Elastic behavior of all-silica Ferrierite:

HP-induced hydration of a “hydrophobic” zeolite

Rossella Arletti1, Simona Quartieri2, Giovanna Vezzalini3

1Dipartimento di Scienze della Terra, Università di Torino, Torino, Italy,

2Dipartimento di Fisica e di Scienze della Terra, Università di Messina, Messina, Italy

squartieri@unime.it

3Dipartimento di Scienze Chimiche e Geologiche, Università di Modena e Reggio Emilia, Modena,

Italy

Keywords: All-Silica Ferrierite, high pressure, hydration, in-situ synchrotron X-ray powder

diffraction.

Introduction

The behavior of water confined to spaces of nanoscopic dimensions is an important issue in

many areas of science and technology [1]. The special situations in which the confining substrates

are hydrophobic have attracted great interest in the past decade [2]. The confinement of water

molecules inside the cavities of high silica zeolites can be obtained under pressure using an aqueous

solution as pressure transmitting medium.

The high-pressure studies performed on zeolites using pore penetrating aqueous solutions, as

P-transmitting media, demonstrated the so called Pressure-Induced Hydration effect (PIH), an

interesting phenomenon in which the water content inside the zeolite cavities increases (“overhydration”)

in response to the applied pressure, through selective sorption of H2O molecules from

the P-medium [see 3 for a review].

Recently, a number of studies on water intrusion – extrusion on all-silica hydrophobic

zeolites showed that these phases can be hydrated by the application of even moderate pressure (~

0.1 GPa) [4,5]. However a structural characterization of the water-loaded systems is still lacking.

In this paper the HP-behavior of an all-silica ferrierite (s.g Pnnm, a=14.0690(8) Ǻ, b=

7.4177(3) Ǻ, c= 18.708(1) Ǻ, V = 1952.3(2) Ǻ3, compressed with two different aqueous media, is

presented and the structural features of the HP-hydrated phase are discussed.

Experimental

The all–silica ferrierite was synthesized following the procedure reported by Rakoczy et al.

[6]. The HP SR-XRPD experiment was performed at the BM01 beam line (European Synchrotron

Radiation Facilities, Grenoble, France) with a fixed wavelength of 0.697 Ǻ and an image plate

detector, using modified Merril-Bassett DACs. Pressure was calibrated using the ruby fluorescence

method on the non-linear hydrostatic pressure scale.

Two different experiments were performed: 1) using a mixture of methanol-ethanol-water

(m.e.w.) in 16:3:1 ratio from Pamb to 8 GPa ; 2) using a mixture ethanol-water (e.w.) in 1:3 ratio

from Pamb to 1.7 GPa (the low pressure reached is due to ice crystallization). One-dimensional

diffraction patterns were obtained by integrating the two dimensional images.

Structural refinements were performed by Rietveld profile fitting up to 1 GPa in e.w. and up

to at 0.2 GPa in m.e.w. (the data quality of the higher pressure patterns being too low for

refinement). The cell parameters were refined for the whole investigated pressure range in both

experiments.

219

Results and discussion

Figure 1 shows the variations of the cell parameters as a function of pressure for the two Ptransmitting

media. The total variation are Δa= -5.8%, Δb= -5%, Δc= -7.1, ΔV= -16.9 and Δa= -

1.4%, Δb= -0.9%, Δc= -1.1, ΔV= -3.4 for the m.e.w. and e.w. experiments, respectively.

The structural refinements indicated the presence of extraframework species even at the

lowest pressure investigated in both experiments. In the zeolite complessed in e.w., a chain of

water (w.) and ethanol molecules (e.) running along the 10 mR and 6mR ferrierite channels were

localized even at 0.2 GPa, accounting for a total of 5 w. and 3.6 e. The HP-induced increase of the

occupancy factors of the localized sites leaded a total load of 10 w. and 4 e. at 1 GPa (Figure 2).

The refinement at 0.2 GPa of ferrierite compressed in m.e.w. allowed localizing 15.6 w., organized

in similar chains. We cannot exclude the penetration of other species (i.e. methanol or ethanol),

which could be disordered on a number of low occupied sites.

Conclusions

The HP structural investigations of an all-silica ferrierite showed that, in both experiments,

the penetration of water and alcohols is achieved at very low pressure. All the species entering the

pores are arranged in chains running along the central axes of the channels. The interactions among

the extraframework molecular species and the framework oxygen atoms are very weak, due to the

hydrophobicity of the framework walls.

References

[1] Ball, P. Nature 2003, 423, 25.

[2] Chandler, D. Nature 2002, 417, 491.

[3] Gatta GD; Z.Kristallogr. 223,160,2008.

[4] Colligan M, Foster PM, Cheetman AK, Lee Y, Vogt T, Hriljac JA; J. Am. Chem. Soc.

126,12015,2004.

[5] Trzpit M, Rigolet S, Paillaud JL, Marichal C, Soulard M, Patarin J; J. Phys. Chem. B

112,7257,2008.

[6] Rakoczy, R.A., Traa, Y., Kortunov, P., Vasenkov, S., Weitkamp, MMM 104 (2007) 179–184