243

P-1.2-04

Use of zeolitites from Central Italy in an integrated cycle aimed at water and

chemical fertilizers saving (ZEOLIFE - LIFE+10ENV/IT/000321)

M.F. Brigatti1, A. Laurora1, D. Malferrari1, E. Passaglia, G. Vezzalini1

1Dep. of Chemistry and Geology, University of Modena and Reggio Emilia, Modena, Italy,

mariagiovanna.vezzalini@unimore.it

Keywords: zeolitite, chabasite, CEC, water saving, LIFE+

Introduction

The project “ZEOLIFE - Water pollution reduction and water saving using a natural zeolitite

cycle” has been conceived to test an innovative integrated zeolitite application having the aim to

reduce the NH4 content in livestock effluents and correct agricultural soils, with improvement of the

yield and economization of water for irrigation and fertilizers. This project leads to a reduction of

fresh and groundwater pollution and avoids excessive exploitation of the water resource. For further

details visit the website www.zeolife.it.

The first goal of the project was to carry out a chemical and physical, as well as

mineralogical characterization of several zeolitite samples, coming from different quarries located

in Central Italy, in order to select the most suitable raw material to be used throughout the entire

project.

Samples from the following seven localities were analyzed: Sorano (Gr), Sovana (Gr),

Farnese (Vt), Grotte Santo Stefano (Vt), Corchiano (Vt), Nepi (Vt), and Riano (Rm). All the

mentioned localities are the closest to the experimental field (Codigoro, Ferrara); in each quarry

non-marketable material, namely broken blocks or blocks with irregular shape and size, is available.

This material represents an already available reserve of zeolitic tuff that best fit the purposes of this

project.

Besides the technological properties of the raw material, the final choice also took into

account factors of environmental (e.g. carbon footprint) and economic (e.g, cost, full and immediate

availability) concern.

Experimental

In order to obtain representative samples from each examined locality, an appropriate

procedure was followed by picking out a total amount of 10 kg of raw material from different points

of the quarries. The collected material was accurately ground, and repeatedly quartered until

obtaining the needed sample amount.

Quantitative mineralogical analyses were carried out using the Rietveld method via the

General Structure Analysis System (GSAS) software package [1], combined with the Reference

Intensity Ratio (RIR) method for the determination of the amorphous phase [2].

Whole rock chemical analysis was carried out on pressed pellets via a wavelength-dispersive X-Ray

Fluorescence (XRF). Loss On Ignition (LOI) was determined by sample heating in a oven at

1100°C. CEC determination of exchanged Ca2+, Mg2+, Na+, and K+ cations was achieved via

Atomic Absorption Spectrometer (AAS) measurements. Apparent density was determined as the

ratio between the mass of ground sample which fills a measuring cup in loose conditions and the

volume of the cup. Water retention was determined using a modified Campbell’s methods [3].

Results and discussion

As demonstrated by plenty of experimental scientific works (e.g., [4] for a review),

chabazite is very effective not only in NH4 uptake from swine manure, but also in successive

controlled NH4 release in soils. Other zeolite species, such as phillipsite, have great potential for

244

NH4 adsorption and retention, but not the same capacity as chabazite in exchanging NH4 with

circulating solutions and plant root systems in soils.

A comparison between samples from studied quarries is reported in Fig. 1. As can be

observed the Sorano zeolitite shows the best features (e.g., high zeolite content and high CEC).