P-2.2-02

Dehydration dynamics of levyne: evidence for a new zeolite topology

Rossella Arletti1, Simona Quartieri2, Giovanna Vezzalini3, Fernando Cámara1

1Dipartimento di Scienze della Terra, Università di Torino, Torino, Italy, rossella.arletti@unito.it

2Diartimento di Fisica e di Scienze della Terra, Università di Messina, Messina, Italy

3Dipartimento di Scienze Chimiche e Geologiche, Università di Modena e Reggio Emilia, Modena,

Italy

Keywords: Levyne, dehydration mechanism, new topology, in-situ synchrotron X-ray powder

diffraction, single-crystal X-ray diffraction

Introduction

Knowledge of the structural modifications induced by temperature in zeolites and of their

stability fields is of prime importance to assess zeolite persistence and effectiveness in their

technological applications. Some porous materials, when completely dehydrated, undergo irreversible changes in the framework topology. In general, these changes are due to the strain induced by migration of cations - initially located in the channels and surrounded by water molecules - to achieve a better coordination with framework anions after the water release.

Notwithstanding the spread interest for porous materials with levyne topology (LEV), their

thermal behavior and stability have not been studied in detail up to now. In this work, the thermal

induced structural modifications of a natural levyne from Fagridalur (Iceland) (Ca7.8

Na2.2K1.1Al19.8Si31.2O108⋅51H2O, a= 13.3619(4) Å, c= 22.8820(1) Å, V = 3538.0(3) Å3, s.g. R-3m) were studied by both temperature-resolved synchrotron X-ray powder diffraction (SR-XRPD), and by conventional-source high-temperature single crystal X-ray diffraction (SC-XRD). LEV framework consists of stacking of 6-rings perpendicular to [0001] (6mR) in the sequence AABCCABBC [1]. Levyne cages are confined by two pairs of D6R and contain the non-framework cations and water molecules. A three-dimensional channel system, confined by 8-membered rings, runs perpendicular to [0001].

Experimental

The temperature-resolved SR-XRPD experiment was performed at the GILDA beam line

(European Synchrotron Radiation Facilities, Grenoble, France). The patterns were collected every

25°C from room-T to 680°C on an image plate detector MAR345. A total of 32 diffraction images

were collected and integrated using Fit2D software. On selected 15 patterns, a complete structural

refinement was performed by means of Rietveld method. After 2 weeks of exposure to air, a powder

patter was collected on a laboratory powder diffractometer equipped with a capillary spinner (CuKα

radiation, Θ/Θ Bragg Brentano geometry, 0.02 step on a angular range 3-100° 2Θ) to test the

rehydration of the sample after the heating cicle.

SC-XRD experiments were performed at the CNR IGG (Pavia) at room-T, 30, 100 and 250 °C,

using a Philips PW1100 four-circle automated diffractometer, equipped with a microfurnace (MoKα

radiation at 30 mA/50 kV - 0.5 mm collimator - θmax =29°).

Results and discussion

Figure 1 reports the behavior of the cell parameters as a function of temperature. Below 100°C

we observe an increase of a lattice parameter, a decrease of c and a very low volume reduction (<1%). Between 100 and 295°C, a decreases and c increases, accounting for a V reduction of ∼ 2%. At 300° a new phase (B) occurs. This phase has the same space group of the original levyne, but shows a smaller volume, as a consequence of the a shortening. The two phases coexist up to 400°C, while at higher temperature only levyne B is found. 110

Figure 1: Cell parameter variation vs temperature

Water is released from the very first stage of heating up to 283°C; as a whole, 26 water molecules are lost. Dehydration induces the cation migration toward the framework oxygen atoms, so to achieve a better coordination. In particular, the calcium cations occupying site C2 (originally coordinated only to water molecules) migrate in the 6mR.

The structure refined at 458°C (levyne B) is completely dehydrated. The new framework is constituted by 50% of the original framework and 50% of a new topology (Figure 2) formed by the breaking of the oxygen bridges in t e D6R, and the consequent formation of new bridges. The amount of broken bridges, up to the highest investigated temperature, never exceed the 50%.

The new framework consists of a sequence along [0001] of a new zeolitic cage and of two cancrinite cages (Figure 2). This framework – reported in the database of the hypothetical zeolite structures [2] as 166_2_293 – belongs to the ABC-6 family [3] and can be described with the following 6mR sequence: ABABABCBC. The new cage can be described as a 20-hedron formed by fourteen 6mR and by six 4mR. The cations are distributed over 3 new sites: one at the center

of the 6mR shared by the two cancrinite cages, one near the center of the base of the

new cage and one in a 6mR window of the new cage. The phase transition is not

reversible (at least in short time) even if the rehydration is almost complete.

Figure 2- The new framework topology

Conclusions

The high temperature behaviour of natural zeolite levyne was studied by in situ SR-XRPD.

Water loss induces the cation migration toward the framework to obtain a better coordination, forcing the breaking of some T-O-T bridges and the consequent formation of new bonds and of a new structure. The 8mR bidimensional channel system of levyne is absent in the new topology and hence the molecular diffusion should be partially hindered in the dehydrated form.

References

[1] S. Merlino, E. Galli, A. Alberti, Mineral. Petrogr. Mitt. 22 (1975) 117-129.

[2] M.D. Foster and M.M.J. Treacy http://www.hypotheticalzeolites.net

[3] Ch. Baerlocher, W.M. Meier, D.H. Olson, Atlas of Zeolite Framework Types (2001) Elsevier, The Netherlands.