Fluorenone dye- zeolite L hybrid:

a novel optical material

Gigli L1.,  arletti R2., quartieri S3., vezzalini G1.

1 Department of chemical and Geological Sciences, University of Modena and Reggio Emilia, Italy,

2 Department of Earth Sciences, University of Torino, Italy

3 Department of Earth Sciences- University of Messina, Italy

A major challenge facing humanity is developing renewable source of energy. Following the biological blueprint of the natural photosynthesis is possible design synthetic systems for converting light into stored  energy: the so called artificial antenna systems. The encapsulation of ordered chromophore molecules into one dimensional  zeolite channel systems results in host-guest compounds suitable for the development of  novel optical materials such as lenses, infrared light-emitting diodes (used in telecommunications) or dye nanostructured materials for optical data storage [1]. X-ray powder diffraction study of zeolite K-L loaded with 0.5, 1, 1.5, 2 fluorenone-dye (FL) molecules per unit cell (ZL/FL hybrid) [2], was carried out to understand the functionality of these host-guest systems from the structural point of view. These data evidenced a significant change of the unit cell parameters due to the embedding of FL into the ZL 12-membered channels. The Rietveld refinements revealed that the maximum loading is 1.5 FL molecules per unit cell. A strong interaction between FL carbonyl group and two extraframework  potassium cations is proved by the short bond distances which make this composite very stable.

This work is supported by the Italian MIUR (FUTURO IN RICERCA 2012: ImPACT project  (RBFR12CLQD)

Fig.1 Projection along c axis of the ZL/FL (1 molecule) (A) and ZL/FL (1.5 molecules) composites (B) .

[1] St. Suárez, A. Devaux, J. Bañuelos, O. Bossart, A. Kunzmann and Gion Calzaferri  Properties Adv. Funct. Mater.(2007),17 , 2298–2306. [2]A. Devaux, C. Minkowski, and Gion Calzaferri Chem. Eur. J. 10, (2004), 2391

# Text boxes

B

A